| Nr. ctr. | Temperatu-ra de încălzire, [oC] | Durata de menţinere, [h] | Medii de răcire | Referinţe | Aliaj |
| --- | --- | --- | --- | --- | --- |
| 1. | 1000 | 24 | - | Sade, M., Halter, K. and Hornbogen, E. – The effect of thermal cycling on the transformation behaviour of Fe-Mn-Si shape memory alloys, Progress in Shape Memory Alloys, (Eucken, S. ed.), DGM-Informationsgesellschaft Verlag, Bochum, 1992, 201-212 | Fe-Mn-Si |
| 2. | 1050 | 1-3 | Răcire în trepte: apă-azot lichid | Dubois, B. –Aciers a memoire de forme. Espoir ou realite?, Traitement Thermique, 234, 1990, 27-34 | Fe-Mn-Si |
| 3. | 1200 | 0,5 | Apă | Li Jian and C.M.Wayman – On the mechanism of the shape memory effect associated with γ(cfc) to ε(hcp) martensitic transformations in Fe-Mn-Si alloys, Scripta Metallurgica et Materialia, Vol.27, pp. 279-284 | Fe-32Mn-6Si-0,04C-0,05Nb |
| 4. | 1100 | 4 | Apă | D. Wang, W. Ji, M. Han, D. Jia, W Liu – Influence of Ausforming on Substructues and Shape Memory Behavior in Fe-28Mn-6Si-5Cr Alloy, Materials Science Forum Vols. 327-328(2000) pp. 263-266 | Fe-28Mn-6Si-5Cr |
| 5. | 1000 | 15 | - | Xiaochun Wu, T.Z. Hsu (Xu Zuyao) – Effect of the Neel temperature, TN, on martensitic transformation in Fe-Mn-Si-based shape memory alloys, Materials Characterization 45 (2000) pp. 137-142 | Fe-Mn-Si |
| 6. | 1000, în Ar | 1 | Ulei, la 99 oC | A. Sato, Y. Yamaji, T. Mori – Phisical properties controlling shape memory effect in Fe-Mn-Si alloys, Acta Metallurgica Vol34. No.2, 287-294, 1986 | Fe-Mn-Si |
| 7. | 1065 | 0,5 | Apă | Edwin R Jones, Jr., T. Datta, C. Almasan, D. Edwards, H.M. Ledbetter – Low Temperature Magnetic Properties of F.C.C. Fe-Cr-Ni alloys: Effects of manganese an Interstitial Carbon and Nitrogen, Materials Science and Engineering 91, (1987) 181-188 | Fe-Cr-Ni |
| 8. | 1200 | 10 | Apă | T Sawaguchi, T Kikuchi and S Kajiwara, The pseudoelastic behavior of Fe–Mn–Si-based shape memory alloys containing Nb and C, Smart Mater. Struct. 14 (2005) S317–S322 | Fe–28Mn–6Si–5Cr–0.53Nb–0.06C |
| 9. | 1230 | 1 | Apă | B.X. Huang, X.D. Wang, Y.H. Rong, L. Wang, L. Jin, Mechanical behavior and martensitic transformation of an Fe–Mn–Si–Al–Nb alloy, Materials Science and Engineering A 438–440 (2006) 306–311 | Fe–23Mn–2Si–2Al |
| 10. | 1200 in argon | 1 | Apă | N. Stanford, D.P. Dunne, Effect of second-phase particles on shape memory in Fe–Mn–Si-based alloys, Materials Science and Engineering A 454–455 (2007) 407–415 | Fe–26Mn–5Si–2Ni |

Tab. 3 Temperaturi de încălzire, duratele de menținere și mediile de răcire, recomandate în literatura de specialitate