| Nr. ctr. | Temperatura de încălzire | Durata de menţinere | Medii de răcire |  | Referinţe | Aliaj |
| --- | --- | --- | --- | --- | --- | --- |
| 1. | 10000C (călire de punere în soluţie) | 0,5 h | Aer |  | Sade, M., Halter, K. and Hornbogen, E. – The effect of thermal cycling on the transformation behaviour of Fe-Mn-Si shape memory alloys, Progress in Shape Memory Alloys, (Eucken, S. ed.), DGM-Informationsgesellschaft Verlag, Bochum, 1992, 201-212 | Fe-30,5 Mn-5 Si |
|  |  |  | Ulei |  |  |  |
|  |  |  | Apă |  |  |  |
|  |  |  | Saramură |  |  |  |
|  | 300-7000C (îmbătrânire) | 20 h | Apă |  |  |  |
|  |  | 30 h |  |  |  |  |
|  |  | 50 h |  |  |  |  |
| 2. | 1070 K | 10 min | Apă |  | Z.Z.Dong, S.Kajiwara, T.Kikuchi, T.Sawaguchi – Effect or pre-deformation at room temperature on shape memory properties of stainless type Fe-15Mn-5Si-9Cr-(0.5-1.5)NbC alloys, Acta Materialia, 53, 2005, 4009-4018 | Fe-15Mn-5Si-9Cr-(0.5-1.5)NbC |
| 3. | 970 K | 10 min | Apă |  | S.Kajiwara – Characteristic features of shape memory effect and related transformation behavior in Fe-based alloys, Materials Science and Engineering 273-275, (1999) 67-88 | Fe-14Mn-6Si-9Cr-5Ni |
| 4. | 9000C | 1 h | Apă |  | D. Wang, W. Ji, M. Han, D. Jia, W Liu – Influence of Ausforming on Substructues and Shape Memory Behavior in Fe-28Mn-6Si-5Cr Alloy, Materials Science Forum Vols. 327-328(2000) pp. 263-266 | Fe-28Mn-6Si-5Cr |
| 5. | 1173 K | 10 min | - |  | Xiaochun Wu, T.Z. Hsu (Xu Zuyao) – Effect of the Neel temperature, TN, on martensitic transformation in Fe-Mn-Si-based shape memory alloys, Materials Characterization 45 (2000) pp. 137-142 | Fe-Mn-Si |
| 6. | 1338 K | 0,5 k | Apă |  | Edwin R Jones, Jr., T. Datta, C. Almasan, D. Edwards, H.M. Ledbetter – Low Temperature Magnetic Properties of F.C.C. Fe-Cr-Ni alloys: Effects of manganese an Interstitial Carbon and Nitrogen, Materials Science and Engineering 91, (1987) 181-188 | Fe-Cr-Ni |
| 7. | 9500C | 1 h | Apă |  | Defa Wang, Daozhi Liu, Zhizhong Dong, Wenxi Liu, Jinming Chen – Improvement of shape memory effect by ausforming in Fe–28Mn–6Si-5Cr alloy, Materials Science and Engineering A315, (2001) 174-179 | Fe–28Mn–6Si–5Cr |
| 8. | 1070 K | 10 min | Apă |  | Takahiro Sawaguchi, Puspendu Sahu, Takehiko Kikuchi, Kazuyuki Ogawa, Setsuo Kajiwara, Atsumichi Kushibe, Masahito Hihashino, Takatoshi Ogawa, - Vibration mitigation by the reversible fcc/ hcp martensitic transformation during cyclic tension-compression loading of an Fe-Mn-Si – based shape memory alloy, Scripta Materialia 54 (2006) 1885–1890 | Fe–28Mn–6Si–5Cr-0.53 Nb-0.06 C |
| 9. | 670 K | 48 k | Îmbătrânire | Apă | S.Kajiwara, D.Z.Liu, T.Kikuchi and N. Shinya – Development of Fe-Mn-Si based shape memory alloys with no necessity of "training"¸Journal de Physique IV, 11 (2001) 199-204 | Fe-28Mn-6Si-5Cr-(0.5-1.5)NbC |
|  | 770 K | 24 h |  |  |  |  |
|  | 870 K | 4 h |  |  |  |  |
|  | 970 K | 2 h |  |  |  |  |
|  | 1070 K | 2 h |  |  |  |  |
|  | 1170 K | 2 h |  |  |  |  |
|  | 1270 K | 2 h |  |  |  |  |
|  | 1370 K | 2 h |  |  |  |  |
| 10. | 6000C | 5 min | Apă |  | N. Van Caenegem, L.Duperey, K.Verbeken, D.Segers, Z.Houbaert, Stresses related to the shape memory effect in Fe–Mn–Si-based shape memory alloys, Materials Science and Engineering A 454–455 (2007) 407–415 | Fe29Mn7Si Fe29Mn7Si5Cr |
|  | 8000C |  |  |  |  |  |
|  | 10000C |  |  |  |  |  |

Tab. 3.1 Temperaturi de încălzire, duratele de menţinere şi mediile de răcire, recomandate în literatura de specialitate pentru tratamentul termic secundar al AMF Fe-Mn-Si-Cr-Ni